[image: image1.jpg]\\\






OSMAFIN AQUABLOCK TRIPLE
Water and oil proofing liquid for personal wear
Application

· Sustaining and providing chemical, oil and water repellency on PPE, medical, textiles.

· Applicable for aramid, polyester, cotton, acrylic fabrics and mixtures thereof.
Properties
· Provides protection against penetration by liquid chemicals on PPE textiles according to DIN EN6530.

· Provides oil repellency on PPE textiles according to AATCC 118/EN ISO 14419
· Sustains spray resistance for 
EN 13034(2005)+A1(2009) part 5.2 rated textiles, tested according to 
ISO 17491-4A (2008): Resistance to penetration by a spray of liquid after 50x,100x wash + impregnation (ISO 15797) 

· Provides alcohol repellency according to AATCC 193.
· No staining on coloured fabrics.
· No deposits in ironers.
Use instructions

Sufficiently rinse the textiles to reduce residual surfactant levels. Dose in the last rinse cycle:

· 15-30 mL/kg dry textiles to sustain repellency effects on proofed garments.
· Use 45mL/kg dry textiles on non- proofed textiles.

Apply under acidic conditions (pH 4-5) followed by a drying cycle at temperatures between 60-135°C. For short drying times (e.g. 3 minutes) a drying temperature of >100°C on the dry textile is recommended.
Waterproofing can also be carried out under low temperature drying conditions with long times e.g. overnight drying in fire brigade drying cabinets.
Composition according EC-directive
None.
Physico-chemical properties 
Density (20 °C):
1.02 g/ml

pH-value (1%):
ca. 5.0
Environment

· Does not contain phosphates, NTA and EDTA.

· Does not contain PFOA and PFOS

· COD-value: 10 mg/kg.

Safety and transport
Not harmful.
Meets European directives on the classification, packaging and labelling of dangerous chemical substances and preparations.

Storage
Use above 5°C.  Store above 0°C and below 40°C. Keep away from direct sunlight.
Packaging
Bottle

20 kg



